Lasing in T-shaped quantum wires with high uniformity

Hidefumi Akiyama*

Institute for Solid State Physics (ISSP), University of Tokyo, and CREST, JST,

5-1-5 Kashiwanoha, Kashiwa, Chiba 277-8581, Japan.

High-quality T-shaped quantum-wire (T-wire) lasers are fabricated by cleaved-edge overgrowth with the molecular beam epitaxy on the interface improved by a growth-interrupt high-temperature anneal [1]. We achieved ground state lasing in single-quantum-wire lasers (T < 60K) [2,3] as well as 20-quantum-wire lasers (T < 120K) [4] by optical pumping. The wires tend to lase in a single mode at energy with a relatively small shift. Lasing threshold of T-wires was lower than that of quantum wells formed in the same samples. Near field pattern of the T-wire laser shows a very good circular shape [5].

Micro-photoluminescence (PL) and PL excitation (PLE) spectroscopy at 4K reveals unprecedented high quality of the wires, and structures of one-dimensional (1-D) free excitons and 1-D continuum states [6]. Transmission experiments have shown that modal absorption at 1D exciton peak at 4 K is fairly large (90/cm for a single T-wire) [7].

At high pumping levels, PL at 4K evolves from a sharp free exciton peak to a red-shifted PL band with symmetric broadening. The lasing energy is about 5 meV below the free exciton, and is on the red-shifted broad PL band. The evolution of this PL band suggests formation of Coulomb-correlated electron-hole plasma [3,4]. Recent measurements of gain spectra via the Cassidy’s method (a modified method of the Hakki-Paoli method) strongly support this assignment [8]. It is concluded that origin of the laser gain is the 1D electron-hole plasma with strong Coulomb correlations.

Additional experiment of PL and PLE spectroscopy for a modulation-doped single quantum wire with a gate to tune 1-D electron density [9] has shown various features (charged excitons, band-gap renormalization, Fermi edge singularity, and so on) to be related to many-body optical response of 1D carriers. All experimental results on doped and undoped T-wires seems to indicate importance of Coulomb interactions among carriers.

[1] M. Yoshita et al., JJAP 40, L252 (2001); APL 81, 49 (2002); J. W. Oh et al., APL 82, 1709 (2003). [2] Y. Hayamizu et al., APL 81, 4937 (2002). [3] M. Yoshita et al., ICPS2004. [4] H. Akiyama et al., PRB 67, 041302(R) (2003). [5] Y. Takahashi et al., APL 83, 4089 (2003). [6] H. Itoh et al., APL 83, 2043 (2003); H. Akiyama et al., APL 82, 379 (2003). [7] Y. Takahashi et al., QELS2004. [8] Y. Hayamizu et al., ICPS2004. [9] T. Ihara et al., ICPS2004; H. Akiyama et al., SSC 122, 169 (2002).

(*) Also a visiting scientist at Bell Laboratories, Lucent Technologies.